# SECTION 10505 (10 51 13)

## METAL LOCKERS

GENERAL

SECTION INCLUDES

Extent of metal lockers and related accessories as indicated on drawings.

See schedules at the end of this section for types of lockers.

RELATED SECTIONS

Section 01572-Construction and Waste Management

Division 3 for concrete base for lockers.

Division 6 for wood sleepers.

SUBMITTALS

Product data and installation instructions for metal locker units.

Recycled Content:

Indicate recycled content; indicate percentage of pre-consumer and post-consumer recycled content per unit of product.

Indicate relative dollar value of recycled content product to total dollar value of product included in project.

If recycled content product is part of an assembly, indicate the percentage of recycled content product in the assembly by weight.

If recycled content product is part of an assembly, indicate relative dollar value of recycled content product to total dollar value of assembly.

Color:  Samples on squares of same metal to be used for fabrication of lockers.

Shop Drawings:  Show metal lockers in dimensioned relation to adjacent surfaces.  Show lockers in plans, elevations, sections, and details, method of installation, fillers, trim, base, and accessories.  Include locker numbering sequence information.

Draft of Warranty.

QUALITY ASSURANCE

Uniformity:  Provide metal lockers that are standard products of single manufacturer, with interchangeable like parts.  Include necessary mounting accessories, fittings, and fastenings.

WARRANTY

Manufacturer is to provide a minimum Lifetime warranty covering all defects in materials and workmanship.

PROJECT CONDITIONS

Do not deliver metal lockers until building is enclosed and ready for locker installation.  Protect from damage during delivery, handling, storage, installation, and until occupancy.

MAINTENANCE

Extra Materials:  Furnish extra materials that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

Full-size units of the following metal locker hardware items equal to 10 percent of amount installed for each type and finish installed, but no fewer than five units:

Hooks.

Identification plates.

As recommended by locker manufacturer.

PRODUCTS

MANUFACTURERS

Manufacturer:  Subject to compliance with requirements, provide products of one of the following:

Art Metal Products.

DeBourgh Mfg Co.

List Industries Inc.

Lyon Workspace Products, LLC.

Penco Products, Inc.

Republic Storage Systems Company.

MATERIALS

All metal locker products are to contain recycled content.

Sheet Steel:  Mild cold-rolled prime grade steel, free from buckle, scale, and surface imperfections.

Hardware:  Hooks of cadmium-plated or zinc-plated steel or cast aluminum.

Handle:  Stainless Steel recess handle.

FABRICATION, GENERAL

Construction:  Fabricate lockers square, rigid, and without warp, with metal faces flat and free of dents or distortion.  Make exposed metal edges safe to touch.  Weld frame members together to form rigid, one-piece structure.  Weld joints and connections.  Grind exposed welds flush.

Finishing:  Chemically pretreat metal with degreasing and phosphatizing process.  Apply baked-on enamel finish to all surfaces, exposed and concealed, except plates and nonferrous metal.

Color:  Provide locker units in color(s) selected by Project Consultant from manufacturer’s standards.  Concealed parts may be manufacturer’s standard neutral color.

LOCKER UNITS

All welded unibody construction.

Body:

Fabricated back, sides, top and bottoms of minimum 16-gage solid rolled sheet steel.

or

Frame/Vertical Panels:  13 gage, 1/2 inch flattened expanded metal frame by 16 gage Hollow T tubular sections and channel frame members designed to enclose all 4 edges of the side panel with the entire assembly MIG welded to form a rigid frame for each locker.  The channel frame members are welded to the front and rear vertical frame members to create and anchor bearing surface of 1-1/4 inches wide and by the depth of the locker at each side panel.

Door:  One-piece, minimum 14-gage solid sheet steel with full height door 18 gage reinforcing. Fabricate to swing 180 degrees.

Ventilation:  Provide doors with secure vents with 20 percent ventilations minimum.

Backs are to be 18 gage solid back.

Latch:  Recessed, 22 gage stainless steel cup and handle, shaped to receive padlock, to be pry-resistant, 11 gage single point non-moving positive securely welded to frame.  Provide rubber bumpers latch side.

Hinges:

3-1/2 inches long, 13 gage, 7-knukle, pin type, securely riveted to frame and welded to the door.  Doors shall be secured to frame with a minimum of 2 tamper resistant rivets per hinge.  Provide 3 hinges for doors 48 inches and higher, and 2 hinges for doors less than 48 inches.

Provide a continuous hinge on box lockers or a minimum of 2 hinges.

Latch assembly:  Provide 22 gage stainless steel recessed to receive padlock.  The recessed pan shall be deep enough to have the lock be flush with the outer door face.  Latch to be pry resistant.  Shall be single point non-moving positive latch securely welded to frame.  Provide rubber bumper latch side.

LOCKER ACCESSORIES

Equipment:  Furnish each locker with the following items, unless otherwise shown:

Hooks (36 inch and taller Units):  One double-prong hook and not fewer than 2 single-prong wall hooks.

Number Plates:  Manufacturer’s standard etched, embossed, or stamped, nonferrous metal number plates with numerals not less than 3/8 inches high.  Number lockers in sequence as directed by Architect.  Attach plates to each locker door, neat top, centered, with at least 2 fasteners of same finish as number plate.

Continuous Slopping Tops:  Not fewer that 18 gage sheet steel, approximately 25 degree pitch, in lengths as long as practicable but less than lockers.  Provide closures at ends.  Finish shall match lockers.

Provide sloping tops with upper portion of locker tier only.

Filler Panels:  Provide filler panels where indicated, of not less than 16 gage steel sheet, factory fabricated and finished to match locker units.

Locker Room Benches:  Manufacturer’s standard laminated maple hardwood tops 9-1/2 inch wide by 1-1/4 inch thick, in lengths as indicated.  Provide heavy-duty cast iron pedestal supports not more than 6’-0” o.c. with provisions for fastening to the floor and securing to the bench.  Furnish all anchorages.  Apply standard clear coating to bench tops. Apply baked enamel finish on pedestals.

Provide appropriate ADA compliant lockers and benches as indicated on drawings.  Provide appropriate signage for locker doors.

EXECUTION

INSTALLATION

Install metal lockers at locations shown in accordance with manufacturer’s instructions for plumb, level, rigid, and flush installation.

Space fastenings about 48 inches o.c., unless otherwise recommended by manufacturer, and apply through backup reinforcing plates where necessary to avoid metal distortion, using concealed fasteners.

Install trim, sloping top units, and metal filler panels and end panels, using concealed fasteners.  Provide flush, hairline joints against adjacent surfaces.

ADJUST AND CLEAN

Adjust doors and latches to operate easily without binding.  Verify that integral locking devices are operating properly.

Touch up marred finishes, but replace units that cannot be restored to factory-finished appearance.  Use only materials and procedures recommended or furnished by locker manufacturer.

SCHEDULES

Refer to Ed Specs and the drawings for locations, sizes, and configurations.

Typical Locations:

Elementary School:

Food Service Employee Lounge:

Middle Schools:

Custodian Restroom.

Food Service Employee Lounge.

Phys-Ed Dressing Rooms.

High School:

Custodian Restroom.

Family & Consumer Science Culinary Operations.

Food Service Employee Lounge.

Phys-Ed Dressing Rooms.

Phys-Ed Teacher Planning.

Benches:  Provide double width benches the length of locker rooms.

END OF SECTION