# SECTION 02747 (32 18 23.10)

## ASPHALTIC CONCRETE PAVING FOR PLAY COURTS AND TRACKS

- GENERAL

- SECTION INCLUDES

    - Asphaltic Concrete Paving for Playcourts, Tennis Courts and Tracks.

    - Surface Sealer.

    - Wearing Binder or Base Course.

    - RELATED SECTIONS

    - Section 02791-Color Surface for Play Courts.

    - REFERENCES

    - American Association of State Highway and Transportation Officials (AASHTO):

      - AASHTO T-180-74 (82):  Moisture-Density Relations of Soils Using a 10 pound hammer and an 18-inch Drop and 1983 interim revision.

    - American Society for Testing Materials (ASTM)

      - ASTM A615-86, Specification for Deformed and Plain Billet-Steel Bars for Concrete Reinforcement.

    - Florida Department of Transportation (DOT):

      - Standard Specifications for Road and Bridge Construction.

      - QUALITY ASSURANCE

    - Perform work under provisions of State of Florida Department of Transportation "Standard Specifications for Road and Bridge Construction".  Mixing Plant: Conform to State of Florida DOT Standards.

    - Obtain materials from same source throughout.

    - ENVIRONMENTAL REQUIREMENTS

    - Do not place asphaltic when base or surface is wet or when base surface temperature is less than 40 degrees Fahrenheit.

    - JOB CONDITIONS

    - After final rolling, protect newly placed material from traffic by barricades or other suitable methods until it has hardened, and in no case less than 24 hours.

    - After final rolling prohibit vehicular traffic of any kind.  Completed areas shall not be used for storage or staging areas of any kind.

    - PRODUCTS

    - MATERIALS

    - Paving Materials:

      - Fill: Sand and/or rock, containing not over 40 percent rock, 2 inches maximum size.

      - Lime rock Base Course: Miami Oolite Lime rock, 60 percent lime content, free from sand, marl, roots, boulders, and other unsuitable material.

      - Prime Coat:  Cut back asphaltic, DOT grade RC-70 or RC-250.

      - Tack Coat:  Asphaltic Cement, Penetration Grade 85-100 percent or emulsified asphaltic, DOT grade RS-2.

      - Wearing Surface Coarse:  Asphaltic Concrete, Type S-III for track, outside basketball courts, tennis courts.

      - EXECUTION

      - GENERAL

    - Connections to Existing Pavements: Saw cut with joints neat and as inconspicuous as possible.

    - Patching Existing Pavements: Repair existing pavement if damaged or removed due to construction activities as directed by the Owner.

    - EXAMINATION

    - Verify that compacted subgrade is dry and ready to support paving and imposed loads.

    - Verify gradients and elevations of base are correct.

    - Beginning of installation means acceptance of substrate.

    - PLANT CONTROL

    - Grass and Weed Extermination:

      - Apply weed killer over entire lime rock base course area to be surfaced, prior to the installation of the prime coat.

      - Use Round-Up or approved equal as per manufacturer's recommendations for non-crop areas.  Provide a second application layer around the full perimeter, 2 feet wide, of the paved area.

      - Repeat as required to eliminate plant growth.

      - Coordinate and arrange for owner inspection of areas to be treated during treatment of the surface.

      - PAVING INSTALLATION

    - Subgrade Preparation:

      - Bring top of subgrade between outer limits of base course to a surface conforming to grades, lines and cross sections as indicated on drawings.

      - Machine compact existing subgrade to 98 percent of maximum dry density as determined by AASHTO T-180.

      - Provide additional fill where required under paved areas and compact as specified above.  Apply in layers not to exceed 12 inches.

      - Stabilize all subgrade material within the limits indicated on the drawings, which provide a Lime rock Bearing Ratio of not less than 40 under provisions of Section 160 of the DOT Standard Specifications.

      - After the subgrade has been properly shaped (and stabilized), bring it to a firm unyielding surface by rolling or hand tamping.

        - If the subgrade material does not contain sufficient moisture at the time of rolling to insure proper compaction, water as directed by the Owner and then compact.

        - Permit subgrade material containing excess moisture to dry to the proper consistency before compacting.

        - Compact the top 12 inches of the subgrade, including cut and fill sections, to a density of not less than 100 percent of the maximum density as determined by AASHTO T-180.

      - After the substrate has been prepared, maintain it free of ruts, depressions, and damage resulting from the hauling and handling of any material, equipment, tools, etc.

        - Construct and maintain ditches or drains along the completed subgrade section to keep it from becoming waterlogged.

        - Just before the base course is laid, test the subgrade as to crown and elevation.

        - The elevation of the subgrade is to be within 1/4 inch of the required elevation.

    - Base Course:

      - Base Course Construction: Conform to DOT Standard Specification, Section 200.  Construct base course on the prepared subgrade conforming to the lines, grades, notes, and cross sections indicated in the Drawings.

      - Spread base material uniformly, scarify and then shape to produce required grades and cross sections after completion.

      - Rough grade, roll, finish grade and then water and roll base until a thoroughly bonded, unyielding, and compact base is obtained.

      - Thickness after compaction:  Six inches minimum unless otherwise indicated.

      - Compact base course to 98 percent maximum density under provisions of AASHTO T-180.

      - Maintain grades shown on drawings.  Correct all irregularities greater than 1/4 inch in 10 feet.

    - Prime Coat:

      - After base course has completely cured and is dry, remove loose material, dust, dirt, and foreign material, which might prevent bonding of prime coat.

      - Apply prime coat at rate of not less than 1 gallon per 10 square yards.

    - Tack Coat:

      - If the primed base has become dirty and cannot be cleaned, or in areas where prime coat has cured and lost bonding ability, apply a tack coat at rate of 1 gallon per 10 square yards.

      - When weather conditions delay installation of wearing surface, seal the surface with emulsified asphaltic at the rate of 2 gallons per 10 square yards.

    - Surface Course:

      - Place to a minimum thickness of 1 inch unless otherwise indicated. Apply when surface is dry and weather conditions are suitable.

      - Place asphaltic concrete at an average rate of 20 square yards per ton. Spread mixture with mechanical spreaders.

        - Seal roll mixture using tandem steel rollers weighing between 5 and 12 tons and following as close behind spreader as possible.

        - Roll with self-propelled pneumatic tire rollers covering every portion of surface with at least 12 passes.

        - Roll asphaltic in the direction of water drainage sheet flow.  Seams in the finished surface resulting from rolling operations shall be parallel to the direction of drainage sheet flow.

        - Final roll surfaces with 8 to 12 ton tandem steel rollers before temperature of mixture has dropped below 140 degrees Fahrenheit. Continue rolling until all roller and tire marks have been eliminated.

      - Saw cut all edges straight and true.

      - Finish surface not to vary more than 1/4 inch in 10 feet when measured in any direction. Provide for free drainage of water.

      - Rework, including pavement removal and replacement, areas that pocket water to a depth of more than 1/16 inch.

      - INSTALLATION TOLERANCES

    - In the presence of the Owner, flood the resurfaced area to confirm that all water drains off properly with no "bird baths".

    - Rework areas that pocket water to a depth of more than 1/16 inch until proper slope for the section and cross drainage is achieved.

    - FIELD QUALITY CONTROL

    - Perform field inspection and testing under provisions of Section 01450, “Quality Control”.

    - Include inspection and testing of sub grade and base course to verify obtained densities after compaction; and to verify thickness of completed base and surface courses.

END OF SECTION