# SECTION 02791 (32 18 23.46)

## COLOR SURFACE FOR PLAY COURTS

- GENERAL

  - SECTION INCLUDES

    - Surface color coating systems for asphalt tennis court, basketball courts, elementary school play courts.

    - Court marking and line painting for play courts and asphalt tracks.

  - RELATED SECTIONS

    - Section 01572-Construction Waste Management.

    - Section 02747-Asphalt Paving for Play Courts.

  - REFERENCE STANDARDS

    - American Sports Builders Association (ASBA).

    - National Federation of State High School Associations (NFHS).

    - United States Tennis Association (USTA) Rules of Tennis.

  - SUBMITTALS

    - Submit manufacturer’s literature, specifications, installation instructions and maintenance instructions.

    - Product:  Products specified are to establish a standard of quality and are not intended to limit or exclude other products.  Comparable materials by other manufacturers may be submitted under provisions of Section 01630, “Product Substitution Procedures.”

    - Submit color samples of color coating.

    - Test Reports: Submit independent test results for solar reflectance index (SRI) minimum 29.

  - DELIVERY, HANDLING, and STORAGE

    - Store Materials under provisions of Manufacturer’s instructions:  Protect from extremes of weather, temperature, moisture and other damage.

    - Deliver materials to site in manufacturer’s original sealed containers with proper labels attached.

  - WARRANTY

    - Provide warranty against defects in the materials and workmanship for a period of 1 year from the date of final acceptance.

  - QUALITY ASSURANCE

    - Manufacturer’s Qualifications:  Submit documentation that manufacturer had been regularly engaged in the production of products as specified for a minimum of 5 years.

    - Installer’s Qualifications:  Firm regulatory engaged in construction or re-surfacing of all weather tennis courts, play courts, tracks, or similar athletic surfaces.

      - Submit documentation of minimum 4 years previous experience in construction or resurfacing of all weather tennis courts, play courts, tracks, or similar athletic surfaces in the form of a list of past installations including:

        - Facility Owner.

        - Location of court/surface.

        - Size and type of court/ surface.

        - Year construction or re-surfacing was performed.

    - Manufacturer’s Inspection

      - Manufacturer’s Inspection:  Conduct an inspection with representatives of the Court surfacing manufacturer in the presence of the Owner.

      - Manufacturer’s Installation Report:  Submit results of the Manufacturer’s Inspection to the Owner.  Include noted deficiencies and recommendations for corrective action.

- PRODUCTS

  - ACCEPTABLE MANUFACTURERS

    - California Products Corporation-Fortified Plexipave systems.

    - Nova Sports U.S.A-Novaplay System.

    - SportMaster-ColorPlus Pro System.

    - Substitutions:

      - Will be considered by the Project Consultant and Owner when submitted per requirements of Division-0, Division-1, and Section 01630-Product Substitution Procedures.

  - MATERIALS

    - Crack Filler:  Acrylic.

    - Court Patch Binder:  Acrylic

    - Acrylic Resurfacer.

    - Acrylic Color Coating.

    - Line marking primer and Line Paint.

    - ALL MATERIALS SHALL BE PROVIDED BY ONE MANUFACTURER

    - Water:  Clean, fresh, and portable.

    - Note:  All materials and striping must conform to referenced standards.

  - MATERIAL LIMITATIONS

    - Products containing asbestos are strictly prohibited.

- EXECUTION

  - WEATHER LIMITATIONS

    - No application will be conducted on a wet surface to receive color coating, or when rainfall or high humidity is imminent.

    - Install play court surfaces only when the temperature is 55 degrees Fahrenheit and rising.

    - Do not install play court surfaces if the play court’s surface temperature exceeds 140 degrees Fahrenheit.

  - EXAMINATION

    - Examine asphalt surfaces to receive color coating system.

    - Verify that courts meet the referenced standards.

    - Do not begin surface preparation or applications until unacceptable conditions are corrected.

  - SURFACE PREPARATION

    - Protect adjacent surfaces and landscaping from contact with the asphalt court surface color coating system.  Maintain protection for duration of tennis court resurfacing.

    - Asphalt substrate: remove dirt, dust, debris, oil, grease, vegetation, loose materials and other surface contaminant which could adversely affect applications of coating system per manufacturer’s instructions.

    - Cure new asphalt a minimum of 14 to 30 days before application of surface color coating system.

    - Inspect the entire play court area for cracks, minor depressions, and irregularities.  Flood courts with water to check for depressions.

    - Ensure necessary repairs and surface cleaning are completed prior to the application of surfacing materials:

      - Fill cracks, depressions and surface defects   with acrylic based crack filler according to manufacturer’s instructions.

      - Level depressions deeper than 1/16 inch:  Fill depressions with Court Patch Binder according to manufacturer’s instructions.

    - On existing courts, preparation is to follow manufacturer’s instructions. Surface Variations:  Not more than 1/16 inch in 10 feet measured in any direction after repairs and patching r complete.

    - All mixes and application methods: under strict provisions of the manufacturer’s printed instructions.

    - Trim edge of sod along perimeter of existing courts to provide straight clean aged along newly finished surface.

  - FINISH COURSE PREPARATION

    - Apply 2 or more applications of acrylic resurfacer to the substrate surface until all asphalt porosity is eliminated.  Apply acrylic resurfacer at a consistent rate. And according the manufacturer’s specifications. Mix the materials in accordance with manufacturer’s instructions.

    - Visible asphalt porosity after application of resurfacer:  None permitted.

  - APPLICATION OF COLOR COATING

    - Apply a minimum of 2 coats of color coating to prepared surfaces in accordance with manufacturer’s instructions.

    - No application shall be covered by a succeeding application until thoroughly cured and dried.

    - Color Base with all mixes for color finish: follow strict recommendations of product manufacturers.

    - The finished surface: have a uniform appearance and be free from ridges and tool marks.

  - LINE MARKINGS

    - Line marking paint is to be from the same manufacturer(s) as colored surface manufacturer(s).

    - Lay out court line markings in accordance with appropriate governing body and SBBC requirements.

    - Apply acrylic line markings primer, after masking tape has been laid, to seal voids between masking tape and court surface to prevent bleed-under when line paint is applied.

    - Apply a minimum of 1 coat of acrylic line paint in accordance with manufacturer’s instructions.

  - PROTECTION

    - Erect appropriate temporary barriers to protect the coatings during drying and curing periods.

    - After finish coat and line marking, prohibit and protect from vehicular traffic of any kind.  Completed areas shall not be used for storage or staging areas of any kind.  Any damage shall be repaired at no cost to the owner.

  - CLEAN- UP

    - Remove all containers, surplus materials and debris and dispose of in accordance with the General Contractor’s Waste Disposal Plan and/or in accordance with LEED for Schools criteria.  Minimize any waste to go to a landfill.

    - Remove all spills and overruns.

    - Leave site in clean and orderly condition.

  - INSPECTION

    - Contractor: schedule inspection by Owner for all stages of court preparation, surface patchwork and color application work.

    - Conduct an inspection with representatives of the court surfacing manufacturer and the installing contractor in the presence of the owner.

END OF SECTION