# SECTION 02848 (32 17 13)

## PARKING BUMPERS

- GENERAL

  - SECTION INCLUDES

    - Precast concrete parking bumpers and anchor pins.

  - REFERENCES

  - International Organization for Standardization (ISO) 14021–1999; Environmental Labels and Declarations

  - SUBMITTALS

    - Product Data:  Submit product data for all concrete materials, accessories, and admixtures proposed for use including the following information:

      - Recycled Content:

        - Indicate recycled content; indicate percentage of pre-consumer and post-consumer recycled content per unit of product.

        - Indicate relative dollar value of recycled content product to total dollar value of product included in project.

        - If recycled content product is part of an assembly, indicate the percentage of recycled content product in the assembly by weight.

        - If recycled content product is part of an assembly, indicate relative dollar value of recycled content product to total dollar value of assembly.

      - Regional Materials:

        - Sourcing location(s): Indicate location of extraction, harvesting, and recovery; indicate distance between extraction, harvesting, and recovery and the project site.

        - Manufacturing location(s): Indicate location of manufacturing facility; indicate distance between manufacturing facility and the project site.

        - Product Value: Indicate dollar value of product containing local/regional materials; include materials cost only.

- PRODUCTS

  - MATERIALS

    - All precast products are to contain recycled steel reinforcement, recycled aggregates and materials such as fly ash and granulated ground blast-furnace slag.

    - Provide 6 foot long reinforced precast parking bumper units with two 5/8-inch diameter precast holes for anchor pins.  Reinforcing shall be one No.4 diameter steel reinforcing bar.

    - Anchor Pins:  Plain or deformed No. 4 diameter steel reinforcing bars, 12 inches long, conforming to ASTM A 615, Grade 40.

- EXECUTION

  - INSTALLATION

    - Provide parking bumpers for each stall and anchor pins driven into pavement and made flush with top of bumper.

  - FIELD QUALITY

    - Replace broken or damaged bumpers.

END OF SECTION