# SECTION 02986 (32 01 16.77)

- REPAIR & RESURFACE OF EXISTING PLAY COURTS AND TENNIS COURTS

- GENERAL

  - SECTION INCLUDES

    - Subgrade repairs and patching of existing tennis courts.

    - Tack coat and resurfacing of entire existing asphalt tennis courts.

    - Protective color surfacing for asphaltic tennis courts.

  - RELATED SECTIONS

    - Section 02766-Court Markings for Play Courts and Tennis Courts.

    - Section 02756-Color Surface for Tennis Courts.

  - QUALITY CONTROL

    - The Owner reserves the right to conduct compaction and other testing to verify specification compliance.  Compaction tests and other testing as directed by the Owner under the direction of a Professional Engineer or Testing Laboratory under provisions of Section 01450, “Quality Control”.

    - The Contractor:  Re-execute unsatisfactory work.

- PRODUCTS

  - SUBGRADE MATERIALS FOR REPAIRS

    - Fill:  Sand and/or rock, containing not over 40 percent rock, 2 inches maximum size.

    - Limerock Base Course:  Miami Oolite Limerock, 60 percent lime content, free from sand, marl, roots, boulders, and other unsuitable material.

    - Prime Coat:  Cut back asphalt, DOT grade RC-70 or RC-250.

  - TACK COAT

    - Asphalt cement, Penetration Grade 85-100 for emulsified asphalt, Grade RS-2.

  - WEARING SURFACE

    - Asphaltic Concrete, Type S-III, for track, outside basketball courts and tennis courts.

    - Conform to Florida State Road Department Standard Specifications for Road and Bridge Construction, latest edition.

- EXECUTION

  - PREPARATION OF EXISTING PAVEMENT

    - Grass and Weed Extermination:

      - Apply weed killer over entire asphalt surface to be re-surfaced.

      - Use Round-Up or approved equal as per manufacturer's recommendations for noncrop areas.

      - Repeat as required to eliminate plant growth.

    - Patching and Leveling:

      - Sawcut and remove all cracks/depressions and bubbles in existing pavement surface.

      - Patch and level existing asphalt surfaces to assure proper drainage and watertight uniform surface.

  - SUBGRADE AND BASE REPAIRS

    - Sawcut around potholes, cracks, depressions and bubbles as well as areas indicated to be repaired to provide uniform edge of firm and stable existing pavement.

    - Clean and remove debris and unsuitable base materials including rubbish from sawcut areas.

    - Provide new base materials and prepare base for final surface paving:

      - Base Course:

        - Match elevations of existing and adjacent surfaces.

        - Install, spread, compact limerock base course as to conform to the levels of the existing adjacent asphalt surfaces’ subgrade.

        - Roll, finish grade and then water and roll base until a thoroughly bonded, unyielding, and compact base is obtained.

        - Thickness after compaction: 6 inches minimum unless otherwise indicated.

        - Compact base course to 98 percent maximum density under provisions of AASHTO T-180.

        - Maintain grades shown on drawings.  Correct all irregularities greater than 1/4 inch in 10 feet.

      - Prime Coat:

        - Ensure base course is cured and dry, then remove loose material, dust, dirt, and foreign material, which might prevent bonding of prime coat.

        - Apply prime coat at rate of not less than 1 gallon per 10 square yards.

      - Sanding:

        - Prior to sanding, allow the prime coat to cure for a minimum period of 4 hours.

        - Apply a uniform application of clean sand to the prime coat and roll with traffic roller to cure the prime coat.

      - Tack Coat:

        - Install a tack coat applied with a pressure distributor.  Heat material to a suitable temperature and apply in a thin uniform layer at the rate of 0.1 gallons per square yard.

        - Apply the tack coat sufficiently in advance of the installation of the patch to permit drying but not so far in advance as to allow loss of adhesion as a result of getting covered with dust, dirt, or other debris.

      - Asphaltic Patch:

        - Install minimum 1-inch layer of Type III asphaltic concrete to a thickness equal to existing asphaltic concrete thickness.

        - Connections to Existing Pavements:  To be neat and inconspicuous as possible.

  - SURFACE INSTALLATION

    - When weather conditions delay installation of wearing surface, protect and seal the surface with emulsified asphalt at rate of 2 gallons per 10 square yards.

    - Wearing Surface:

      - Minimum Thickness:  One inch over entire court area, including all patches and paved areas between courts.

      - Install only when substrate surface is dry and when weather conditions are suitable.

      - Spreading:

        - Spread mixture by mechanical spreader.

        - Hand Spreading:  Use only in areas where machine spreading is inhibited or impracticable.

      - Roller Compacting Sequence:

        - Seal Rolling:  Use tandem steel rollers weighing between 5 tons to 8 tons. Follow immediately behind spreaders.

        - Final Rolling:

          - Use 5 ton to 8-ton tandem steel rollers after the seal rolling is completed.

          - Complete final rolling before the asphalt mix temperature has dropped below 140 degree Fahrenheit.

          - Continue final rolling until all roller marks have been eliminated.

          - Trim all open edges straight.

  - INSTALLATION TOLERANCES

    - Finished surface:  Slope surface uniformly to drain with no variance of more than 1/16 inch in 10 feet when measured in any direction.

    - In the presence of the Owner, flood the resurfaced area to confirm that all water drains off properly with no "bird baths".

    - Rework areas, including pavement removal and replacement that pocket water to a depth of more than 1/16 inch until positive drainage is achieved.

END OF SECTION