# SECTION 02987 (32 01 18)

## RESURFACING OF EXISTING TRACKS

- GENERAL

- SECTION INCLUDES

    - Cleaning, patching and treatment of existing surfaces.

    - Seal coating.

    - Tack coating and asphalt wearing course application.

    - Polyurethane bound color surface.

    - RELATED WORK

    - Section 02747-Asphaltic Concrete Paving for Courts and Tracks.

    - Section 02791-Color Surface for Play Courts.

    - Section 02951-Asphaltic Concrete Patching.

    - QUALITY CONTROL

    - The Owner reserves the right to conduct compaction and other testing to verify specification compliance.  Compaction tests and other testing as directed by the Owner and under the direction of a Professional Engineer or Testing Laboratory under provisions of Section 01450, “Quality Control”.

    - The Contractor is to re-execute unsatisfactory work.

    - WARRANTY

    - Contractor will provide warranty against defects in material and workmanship for a period of 1 year from date of final project acceptance.

    - MATERIAL HANDLING AND STORAGE

    - Deliver, protect and apply all material as recommended by the manufacturer with proper material handling and application documents and shop drawings.

    - PRODUCTS

    - TACK COAT

    - Asphalt cement, Penetration Grade 85-100 for emulsified asphalt, Grade RS-2.

    - WEARING SURFACE

    - Asphaltic Concrete, Type S-III, for track, outside basketball courts, tennis courts.

    - Conform to Florida State Road Department Standard Specifications for Road and Bridge Construction, latest edition.

    - SYNTHETIC SURFACE

    - Two-component polyurethane compound formed from polyol and isocyanate.  The polyurethane is based on 100 percent methylene diphenyle isocyanate with no fillers.

    - Finished surface for tracks:  12 mm thick peroxide cured rubber granuals of 1 mm – 2 mm in size embedded in polyurethane of premixed UV stabilized wearing course.

    - EXECUTION

    - PREPARATION OF EXISTING PAVEMENT

    - Grass and Weed Extermination:

      - Apply weed killer over entire asphalt surface to be re-surfaced.

      - Use Round-Up or approved equal as per manufacturer’s recommendations for noncrop areas.

      - Repeat as required to eliminate plant growth.

      - Patching and Leveling:

      - Patch and level existing asphalt surfaces to assure proper drainage and to remove cracks, potholes and depressions.

      - Saw cut and remove up to 12 inches of asphalt surrounding any surface cracks, loose or broken asphaltic surfaces, potholes or depressions.  Ensure any unsound asphalt is removed.

      - Repair base course as necessary to provide solid level finished surface.

      - Compact base and apply prime and tack coat.

      - Apply structural course and final wearing surfaces.

      - INSTALLATION

      - Tack Coat:  Apply at rate of 1 gallon per 10 square yards.

      - When weather conditions delay installation of wearing surface, seal the surface with emulsified asphalt at rate of 2 gallons per 10 square yards.

      - Wearing Surface:

      - Minimum Thickness:  1 inch.

      - Install only when substrate surface is dry and when weather conditions are suitable.

      - Spreading:

        - Spread mixture by mechanical spreader.

        - Hand Spreading:  Use only in areas where machine spreading is inhibited or impracticable.

      - Roller Compacting Sequence:

        - Seal Rolling:  Use tandem steel rollers weighing between 5 to 8 tons.  Follow immediately behind spreaders.

        - Final Rolling:

        - Use 5 to 8 ton tandem steel rollers after the seal rolling is completed.

        - Complete final rolling before the asphalt mix temperature has dropped below 140º F.

        - Continue final rolling until all roller marks have been eliminated.

        - Trim all open edges straight.

        - INSTALLATION TOLERANCES

        - Finished surface:  Slope surface uniformly to drain with on variance of more than 1/6 inch in 10 feet when measured in any direction.

        - In the presence of the Owner, flood the resurfaced area to confirm that all water drains off properly with no “bird baths”.

        - Re-work, including removing and replacing, areas that pocket water to a depth of more than 1/6 inch until sections proposed slope and cross drainage is achieved.

END OF SECTION