# SECTION 02987 (32 01 18)

## RESURFACING OF EXISTING TRACKS

GENERAL

SECTION INCLUDES

Cleaning, patching and treatment of existing surfaces.

Seal coating.

Tack coating and asphalt wearing course application.

Polyurethane bound color surface.

RELATED WORK

Section 02747-Asphaltic Concrete Paving for Courts and Tracks.

Section 02791-Color Surface for Play Courts.

Section 02951-Asphaltic Concrete Patching.

QUALITY CONTROL

The Owner reserves the right to conduct compaction and other testing to verify specification compliance.  Compaction tests and other testing as directed by the Owner and under the direction of a Professional Engineer or Testing Laboratory under provisions of Section 01450, “Quality Control”.

The Contractor is to re-execute unsatisfactory work.

WARRANTY

Contractor will provide warranty against defects in material and workmanship for a period of 1 year from date of final project acceptance.

MATERIAL HANDLING AND STORAGE

Deliver, protect and apply all material as recommended by the manufacturer with proper material handling and application documents and shop drawings.

PRODUCTS

TACK COAT

Asphalt cement, Penetration Grade 85-100 for emulsified asphalt, Grade RS-2.

WEARING SURFACE

Asphaltic Concrete, Type S-III, for track, outside basketball courts, tennis courts.

Conform to Florida State Road Department Standard Specifications for Road and Bridge Construction, latest edition.

SYNTHETIC SURFACE

Two-component polyurethane compound formed from polyol and isocyanate.  The polyurethane is based on 100 percent methylene diphenyle isocyanate with no fillers.

Finished surface for tracks:  12 mm thick peroxide cured rubber granuals of 1 mm – 2 mm in size embedded in polyurethane of premixed UV stabilized wearing course.

EXECUTION

PREPARATION OF EXISTING PAVEMENT

Grass and Weed Extermination:

Apply weed killer over entire asphalt surface to be re-surfaced.

Use Round-Up or approved equal as per manufacturer’s recommendations for noncrop areas.

Repeat as required to eliminate plant growth.

Patching and Leveling:

Patch and level existing asphalt surfaces to assure proper drainage and to remove cracks, potholes and depressions.

Saw cut and remove up to 12 inches of asphalt surrounding any surface cracks, loose or broken asphaltic surfaces, potholes or depressions.  Ensure any unsound asphalt is removed.

Repair base course as necessary to provide solid level finished surface.

Compact base and apply prime and tack coat.

Apply structural course and final wearing surfaces.

INSTALLATION

Tack Coat:  Apply at rate of 1 gallon per 10 square yards.

When weather conditions delay installation of wearing surface, seal the surface with emulsified asphalt at rate of 2 gallons per 10 square yards.

Wearing Surface:

Minimum Thickness:  1 inch.

Install only when substrate surface is dry and when weather conditions are suitable.

Spreading:

Spread mixture by mechanical spreader.

Hand Spreading:  Use only in areas where machine spreading is inhibited or impracticable.

Roller Compacting Sequence:

Seal Rolling:  Use tandem steel rollers weighing between 5 to 8 tons.  Follow immediately behind spreaders.

Final Rolling:

Use 5 to 8 ton tandem steel rollers after the seal rolling is completed.

Complete final rolling before the asphalt mix temperature has dropped below 140º F.

Continue final rolling until all roller marks have been eliminated.

Trim all open edges straight.

INSTALLATION TOLERANCES

Finished surface:  Slope surface uniformly to drain with on variance of more than 1/6 inch in 10 feet when measured in any direction.

In the presence of the Owner, flood the resurfaced area to confirm that all water drains off properly with no “bird baths”.

Re-work, including removing and replacing, areas that pocket water to a depth of more than 1/6 inch until sections proposed slope and cross drainage is achieved.

END OF SECTION