# SECTION 04270 (04 23 00)

## GLASS UNIT MASONRY

GENERAL

SUMMARY

Related Sections:

04200-Unit Masonry.

07920-Joint Sealers.

REFERENCES

ASTM International (ASTM):

C144 Specification for Aggregate for Masonry Mortar.

C150 Specification for Portland Cement.

C270 Specification for Mortar for Unit Masonry.

E119 Test Methods for Fire Tests of Building Construction and Materials.

A82	 Specifications for Steel Wire, plain, for concrete reinforcement.

ASTM A153	 Specifications for Zinc Coating (hot-dip) on iron and steel hardware.

Florida Building Code.

American Concrete Institute (ACI):

ACI 530/530.1-99 Building Code Requirements and Specifications for Masonry Structures.

SUBMITTALS

Submit properly identified manufacturer's literature including installation instructions before starting work.

Submit 1 full size glass masonry unit proposed to be an accepted equivalent for testing by the Owner.

QUALITY ASSURANCE

Certification:  Provide certification by a recognized testing laboratory stating that glass block assembly meets a minimum 3/4-hour fire rating for installation in 1-hour walls.

PRODUCTS

MANUFACTURERS

Glass Unit Masonry:

Pittsburgh Corning Corporation (PC).

Substitutions:

Will be considered by the Project Consultant and Owner when submitted per requirements of Division-0, Division-1, and Section 01630-Product Substitution Procedures.

MATERIALS

Glass Blocks:  Units made of clean, colorless glass:

Thickset by PC, Endura, Decora, or Vue pattern with sizes and shapes as indicated on drawings.

Vistabrick by PC or accepted solid glass equivalent with sizes and shapes as indicated on Drawings.

Mortar:

Portland Cement: ASTM C150, Type I, Domestic.

Masonry Cement: ASTM E119, Domestic.

Sand: ASTM C144.

Water: Potable.

Mortar Mix: ASTM C270, type S proportioned by volume:

Prefabricated wire truss type reinforcement is required.  Both horizontal and vertical at not more than 6 inch cc galvanized to meet ASTM A153 Class B-2.  Acceptable manufacturers:

A.A. Wire Products.

Duro Wall.

Hohman of Bernard.

EXECUTION

INSTALLATION

Lay glass masonry units plumb, true to line, with level and accurately spaced courses as indicated on drawings and according to manufacturer's printed instructions.

Comply with Florida Building Code, and ACI 530/530.1

CLEANING

Remove surplus mortar from faces of glass blocks and wipe dry.

Tool joints smooth and concave, before mortar takes final set.

Accomplish cleaning by means of an ordinary household scrub brush having stiff bristles.

Do not use abrasive cleaners (steel wool, wire brush, or acid) when removing mortar or dirt from the faces of glass block.

END OF SECTION