# SECTION 04530 (04 29 00)

## MASONRY PATCHWORK

- GENERAL

  - SUMMARY

    - Related Sections:

      - Section 04200-Unit Masonry.

      - Section 03300-Cast In Place Concrete Reinforcing.

  - REFERENCES

    - Comply with reference requirements of 03300 and 04200.

  - SUBMITTALS

    - Comply with applicable submittal requirements of 03300 and 04200.

  - QUALITY ASSURANCE

    - Submit unit masonry manufacturer's "CM-2" Certificate of Compliance issued by the Florida Concrete and Products Association for each type of unit masonry specified.

    - Certifications: Comply with applicable sections of 03300 and 04220.

  - PROJECT CONDITIONS

    - Environmental Conditions:

      - Temperature: 40 degrees F. minimum and rising.

      - Weather: No application during precipitation.

- PRODUCTS

  - LOAD BEARING AND NON BEARING CONCRETE UNIT MASONRY

    - Weight:  Normal.

    - Size:  Eight inches x 16 inches x 8 inches thick or as indicated on drawings, 2-cell stretcher type.

    - Texture:  Medium.

    - Grade:  ASTM C90; Grade N-2.

  - CONCRETE BRICK

    - Grade:  ASTM C55, Grade N-2.

    - Size:  Appropriate to suit conditions.

  - MORTAR

    - Portland Cement:  ASTM C150, Type I, domestic.

    - Masonry Cement:  ASTM C91, domestic.

    - Sand:  ASTM C144.

    - Water:  Potable.

    - Mortar Mix:  ASTM C270, Type S, 1800psi or Type M, 2500psi. Mix accurately in following proportions by volume.  Mortar type shall be determined by use and location of masonry as per the Florida Building Code, UON on the drawings.

  - REINFORCEMENT

    - Provide horizontal joint reinforcing in each course.

    - Provide ties to existing materials at sides of patch, at each course.

- EXECUTION

  - INSTALLATION

    - Patching

      - Remove existing mortar from new opening.

      - Fill in as required with new concrete masonry units and fresh mortar.

    - Laying Units:

      - Lay masonry plumb, true to line, with level and accurately spaced courses.

      - Keep bond plumb throughout.

      - Where adjustment must be made after mortar has started to harden, remove mortar and replace with fresh mortar.

      - Cut masonry units dry.

      - Joints:  3/8inch thick thickness, strike flush.

  - JOINTING METHODS

    - Lay concrete block with full beds of mortar on vertical and horizontal face shells.

    - Furrowing of mortar is not allowed.

    - Pointing:  Point holes in masonry.  Cut out and point up defective joints.

  - MORTAR FILLED ITEMS

    - Where necessary and where indicated on drawings.

    - Voids around penetrations through block work.

- END OF SECTION