# SECTION 05520 (05 52 00)

## METAL HANDRAILS AND RAILINGS

- GENERAL

  - SECTION INCLUDES

    - Steel pipe handrails, balusters, and fittings.

    - Aluminum tube handrails, balusters, and fittings.

  - RELATED SECTIONS

    - Section 01572-Construction and Waste Management.

    - Section 05500-Metal Fabrications.

  - REFERENCES

  - International Organization for Standardization (ISO) 14021–1999; Environmental Labels and Declarations

  - SUBMITTALS

    - Product Data:

      - Recycled Content:

        - Indicate recycled content; indicate percentage of pre-consumer and post-consumer recycled content per unit of product.

        - Indicate relative dollar value of recycled content product to total dollar value of product included in project.

        - If recycled content product is part of an assembly, indicate the percentage of recycled content product in the assembly by weight.

        - If recycled content product is part of an assembly, indicate relative dollar value of recycled content product to total dollar value of assembly.

    - Properly identified manufacturer’s literature, including shop and erection drawings before starting work.

    - Railing Assemblies or Railing Components:  Submit shop drawings prepared under direction of an Engineer licensed in the State of Florida showing compliance to the Florida Building Code (FBC).

- PRODUCTS

  - MATERIALS

    - All manufactured metal handrails and railings are to contain recycled content.

  - HANDRAIL AND RAILING COMPONENTS

    - Wall Brackets:  Malleable iron or aluminum as manufactured by Julius Blum & Co., Inc., Carlstadt, NJ, or owner accepted equivalent.

      - Material:

        - Type A:  Aluminum, Model #384 for use with aluminum pipe handrail section.

        - Type B:  Malleable iron, Model #382 for use with steel pipe handrail section.

    - Pipe Handrail Sections:

      - Horizontal Members (Handrails):

        - Steel:  1-1/2 inch OD pipe size, thickness per shop drawings, of design and dimensions indicated with smooth bends and welded joints ground smooth and flush.

        - Aluminum:  1-1/2 inch OD pipe size, thickness per shop drawings, alloy 6061-T6 of design and dimensions indicated with smooth bends and welded joints ground smooth and flush.

        - Alternate 1-1/2 inch OD pipe size, thickness per shop drawings, alloy 6061-T6 of design and dimensions indicated with smooth bends and joints using bolted or fastener connections of tamper-resistant fasteners.

        - Horizontal members are to be used only as handrail or guard rail.

      - Vertical Members (Posts):

        - Steel:  1-1/4 inch nominal pipe size, thickness per shop drawings, of design and dimensions indicated with welded joints ground smooth and flush.

        - Aluminum:  1-1/4 inch nominal pipe size, thickness per shop drawings, alloy 6061-T6 of design and dimensions indicated with smooth bends and welded joints ground smooth and flush.

        - Alternate 1-1/4 inch nominal pipe size, thickness per shop drawings, alloy 6061-T6 of design and dimensions indicated with smooth bends and joints using bolted or fastener connections of tamper-resistant fasteners.

      - Design and construct to withstand 200-pound load applied at any point, from any direction, and other loading as per Florida Building Code.

        - Wall brackets and other points of support are shown to indicate general appearance; submit shop drawings to indicate accurate location of necessary brackets and other points of support to show compliance with load requirements.

      - Provide complete with necessary sleeves, brackets, tamper-resistant bolts, and tamper-resistant fastening devices as required for a complete installation.

  - HANDRAIL and RAILING ASSEMBLIES

    - Manufacturers:

      - Aluminum Manufacturing Industries, Inc., Miami, FL.

      - Dixie Metal Products, Inc., Fort. Lauderdale, FL.

      - Largo Aluminum, Key Largo, FL.

    - Assemblies:  800 Series aluminum railing assembly, or accepted equivalent, composed of both solid castings and aluminum extrusions or shapes designed with integrally extruded locking grooves, fastener seams, and other appendages to insure a rigidly constructed assembly.  Railings shall be able to withstand loads and load combinations specified in the Florida Building Code.

    - Fabrication:

      - Intermediate Posts:

        - Size:  Square shaped, composed of two extrusions joined to form a square shape of not less than 2 inch x 2 inch, designed to be mechanically fastened to the top rail channel with approve fasteners using not less than 2 extruded fastener seams.

        - Material:  Alloy 6061-T6.

        - Minimum Wall Thickness:  0.062 inch.

        - Maximum Spacing:  48 inches on center.

      - Corner Posts:  Same as intermediate posts except mechanically attached to top rail using a specially designed aluminum casting.

      - Pickets:

        - Size; Square shaped, 3/4 inch x 3/4 inch mechanically fastened to the top rail channel with approved tamper-resistant fasteners using 2 extruded fastener seams to prevent picket rotation within the top and bottom extrusions.

        - Material:  Alloy 6061-T5

        - Minimum Wall Thickness:  0.062 inch.

        - Spacing:  Equal spacing placed to reject a 4-inch diameter ball.

      - Top Rail:

        - Size:  Oval shaped, 2-5/8 inch x 1 inch mechanically fastened to top rail channel with approved tamper-resistant fasteners at maximum 24 inches on center.

        - Material:  Alloy 6063-T6.

        - Minimum Wall Thickness:  0.062 inch.

      - Top Rail Channel:

        - Size:  Rectangular shaped, 2 inch x 0.438 inch.

        - Material:  Alloy 6063-T6.

        - Minimum Wall Thickness:  0.062 inch.

      - Bottom Rail:

        - Size:  Rectangular shaped, 1.625 inch x 1 inch mechanically fastened to the post with approved fasteners using 2 extruded fastener seams.

        - Material:  Alloy 6063-T6.

        - Minimum Wall Thickness:  0.062 inch.

      - Approved Tamper-Resistant Fasteners:  18-8 stainless steel screws with the head to be tamper-resistant, sized as recommended by the aluminum railing assembly manufacturer.

  - FINISHING

    - Aluminum Handrail and Railing Components and Handrail and Railing Assemblies:

      - Finish with clear anodizing according to Aluminum Association Standard AA-C22-A21.

        - Anodizing:  200R1 clear with a typical coating of 0.15 mil thickness produced in a 15 percent solution of H2S04 at approximately 70 degrees Fahrenheit at 12 amps per square foot.

    - Malleable Iron Handrail and Railing Components:  Finish with paint materials referenced in Section 09900.

  - MISCELLANEOUS

    - Galvanized Metal Repair Compound:

      - Hot Applied:  Federal Specifications 0-G-93.

      - Cold Applied:  Galvaneal”, “Galvicon”, “Z.R.C.”

    - Isolation Coating:  Zinc chromate paint, heavy-bodied bituminous paint, water-white methacrylate lacquer, or acceptable non-conductive tape.

    - Expanding Grout:  Premix Anchoring Cement by Premix-Marbeletite, Miami, FL., or acceptable equivalent.

  - FASTENINGS, ANCHORS, AND BOLTS

    - Provide required cast-in-place or stainless steel self-drilling anchor bolts as indicated or as recommended by the handrail and railing assembly manufacturer, complete with matching washers and nuts.

- EXECUTION

  - INSPECTION

    - Do not proceed with the work of this section until conditions detrimental to the proper and timely completion of the work have been corrected in an acceptable manner.

  - INSTALLATION

    - Erection:

      - Erect metal handrail and railing components and metal handrail and railing assemblies at proper locations and elevations as indicated, plumb, level, in alignment, and not distorted by fastenings.

      - Erect according to accepted shop drawings and manufacturer’s directions or as specified in this section.

    - Supplementary Parts:  Provide as necessary to complete each item.

    - Contact with Dissimilar Materials:

      - Apply isolation coatings where dissimilar metals are in contact or aluminum components contact dissimilar metal or concrete or lime mortar surface.

      - Select coatings appropriate to the condition from materials specified in this section.

    - Expanding Grout:  Apply according to manufacturer’s printed instructions to clean and dust free surfaces to ensure proper mechanical bond.

    - Malleable Iron Handrail and Railing Components:  Paint to match adjacent surfaces.

END OF SECTION