# SECTION 06300 (06 05 73)

## WOOD TREATMENT

- GENERAL

  - SECTION INCLUDES

    - Preservative water-borne treatment of lumber and plywood.

  - RELATED SECTIONS:

    - Section 06100-Carpentry.

    - Section 06400-Architectural Woodwork.

  - REFERENCES

    - AWPAC20-Structural Lumber, fire Retardant Treatment by Pressure Process; American Wood Preservers Association.

    - AWPA C27-Plywood, Fire Retardant Treatment by Pressure Process; American Wood Preservers Association.

    - AWPB-American Wood Preservers Bureau.

    - Department of Defense (DOD), Military Specification:  MIL-L-19140E Lumber and Plywood, Fire Retardant Treated.

  - SUBMITTALS

    - Wood Treatment Data:

      - Submit chemical treatment manufacturer’s instructions for handling, storing, installation, and finishing of treated materials.

      - Preservative Treatment:  For each type specified, including certification by treating plant stating type of preservative solution and pressure process used, net amount of preservative retained and conformance with applicable standards.

      - Water-Borne Treatment:  Include statement that moisture content of treated materials was reduced to levels indicated before shipment to project site.

  - QUALITY ASSURANCE

    - Wood treatment shall comply with:

      - Florida Building Code and Florida Fire Prevention Code.

  - WARRANTY

    - Treated Wood:  Provide manufacturer’s standard lifetime warranty.

- PRODUCTS

  - MATERIALS

    - Preservative Treatment:

      - Where lumber or plywood is specified to be treated, comply with applicable requirements of AWPA Standards C2, Lumber, and C9, Plywood and of AWPB Standards listed.

      - Mark each treated item with AWPB Quality Mark Requirements.

      - Pressure treat aboveground items with water-borne preservatives to comply with AWPB LP2.

      - After treatment, kiln-dry lumber and plywood to a maximum moisture content of 19 percent or less and plywood to a moisture content of 15 percent or less.

      - Treat indicated items and the following:

        - Wood cants, nailers, curbs, blocking, stripping, and similar members in connection with roofing, windows, flashing, vapor barriers, and waterproofing.

        - Wood sills, sleepers, blocking, furring, stripping, and similar concealed members in contact with masonry or concrete.

        - Wood Framing Members:  Within 18 inches above grade.

      - Pressure treat the following with water-borne preservatives for ground contact use complying with AWPB LP22:

        - Wood members in contact with ground.

        - Wood members in contact with fresh water.

      - Pressure treat lumber and plywood for wood foundation systems with water-borne preservatives for ground contact to comply with AWPB FDN standard.

      - Complete fabrication of treated items before treatment, where possible.

      - Inspect each piece of lumber or plywood after drying and discard damaged or defective pieces.

- EXECUTION

  - APPLICATION

    - Place treated lumber and plywood as detailed.

    - Provide inspection access panels for annual inspection of the condition of the structure and the connector per FBC 423.11

END OF SECTION