# SECTION 06300 (06 05 73)

## WOOD TREATMENT

GENERAL

SECTION INCLUDES

Preservative water-borne treatment of lumber and plywood.

RELATED SECTIONS:

Section 06100-Carpentry.

Section 06400-Architectural Woodwork.

REFERENCES

AWPAC20-Structural Lumber, fire Retardant Treatment by Pressure Process; American Wood Preservers Association.

AWPA C27-Plywood, Fire Retardant Treatment by Pressure Process; American Wood Preservers Association.

AWPB-American Wood Preservers Bureau.

Department of Defense (DOD), Military Specification:  MIL-L-19140E Lumber and Plywood, Fire Retardant Treated.

SUBMITTALS

Wood Treatment Data:

Submit chemical treatment manufacturer’s instructions for handling, storing, installation, and finishing of treated materials.

Preservative Treatment:  For each type specified, including certification by treating plant stating type of preservative solution and pressure process used, net amount of preservative retained and conformance with applicable standards.

Water-Borne Treatment:  Include statement that moisture content of treated materials was reduced to levels indicated before shipment to project site.

QUALITY ASSURANCE

Wood treatment shall comply with:

Florida Building Code and Florida Fire Prevention Code.

WARRANTY

Treated Wood:  Provide manufacturer’s standard lifetime warranty.

PRODUCTS

MATERIALS

Preservative Treatment:

Where lumber or plywood is specified to be treated, comply with applicable requirements of AWPA Standards C2, Lumber, and C9, Plywood and of AWPB Standards listed.

Mark each treated item with AWPB Quality Mark Requirements.

Pressure treat aboveground items with water-borne preservatives to comply with AWPB LP2.

After treatment, kiln-dry lumber and plywood to a maximum moisture content of 19 percent or less and plywood to a moisture content of 15 percent or less.

Treat indicated items and the following:

Wood cants, nailers, curbs, blocking, stripping, and similar members in connection with roofing, windows, flashing, vapor barriers, and waterproofing.

Wood sills, sleepers, blocking, furring, stripping, and similar concealed members in contact with masonry or concrete.

Wood Framing Members:  Within 18 inches above grade.

Pressure treat the following with water-borne preservatives for ground contact use complying with AWPB LP22:

Wood members in contact with ground.

Wood members in contact with fresh water.

Pressure treat lumber and plywood for wood foundation systems with water-borne preservatives for ground contact to comply with AWPB FDN standard.

Complete fabrication of treated items before treatment, where possible.

Inspect each piece of lumber or plywood after drying and discard damaged or defective pieces.

EXECUTION

APPLICATION

Place treated lumber and plywood as detailed.

Provide inspection access panels for annual inspection of the condition of the structure and the connector per FBC 423.11

END OF SECTION