# SECTION 07190 (07 26 00)

## VAPOR BARRIER

GENERAL

SECTION INCLUDES

Vapor Barrier is to be installed at all interior slab-on-grade.

RELATED SECTIONS

Section 02200-Earthwork.

Section 03300-Cast-In-Place Concrete.

SUBMITTALS

Submit properly identified manufacturer’s literature before starting work.

QUALITY ASSURANCE

Regulatory Requirements (Latest Editions):  Comply with the requirement of Florida Department of Health and Rehabilitative Services (HRS), Office of Radiation Control as stated in “Radon-Resistant Construction Guidelines for Use in Florida”, and Florida Building Code.

PRODUCTS

MATERIALS

Vapor Barrier:  Ten-mil polyethylene film minimum.

Tape:  Type recommended by vapor barrier manufacturer; except at vertical penetrations, use reinforced duct tape.

EXECUTION

INSTALLATION

Lay vapor barrier over entire area to receive interior slab work.

Lay vapor barrier with seams perpendicular to and lapped in direction of concrete pour.

Seal all joints by lapping 4 inches minimum and tape all joints.

Turn edges up to 4 inches to top of slab.

Where expansion joints are indicated at adjacent vertical surfaces, extend vapor barrier beyond expansion joint filler and turn up to top of slab.

Do not allow screed supports or other items to penetrate vapor barrier.

Extend vapor barrier over surfaces of areas to be protected from vapor or transmission from conditioned space to unconditioned space after placement of insulation.

Seal all joints by lapping 4 inches minimum and tape all joints.

Repair any punctures or tears before placement of finished surface materials.

Continuously tape entire perimeter of vapor barrier to adjacent surfaces; around all pipe penetrations; and vapor membrane joints; to seal and prevent vapor moisture penetration.

PROTECTION

Protect vapor barrier from damage until permanent covering is in place.

Repair punctures and tears in vapor barrier using patches of the material overlapping the puncture or tear a minimum of 12 inches.  Seal with tape.

END OF SECTION