# SECTION 09665 (09 65 16)

## RESILIENT SHEET FLOORING

- GENERAL

  - SECTION INCLUDES

    - Resilient sheet flooring in gymnasium and in locations as shown on the drawings.

    - Rubber base.

    - Installation Accessories.

  - RELATED SECTION

    - 01572-Construction Waste Management.

    - 03300-Cast-in-Place Concrete.

    - 07132-Vapor Protective Waterproofing.

  - REFERENCES

    - American Society of Testing Materials (ASTM).

      - E84-Surface Burning Characteristics of Building Materials.

      - E648-Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Energy Source.

      - E662-Optical Density of Smoke Generated by Solid Materials.

      - F710-Preparing Concrete Floors to receive Resilient Flooring

      - F1859-Rubber Sheet Floor Covering Without Backing.

      - F1861-Resilient Wall Base.

    - GREENGUARD Product Emission Standard for Children & Schools.

    - ISO 14021–1999; Environmental Labels and Declarations

    - Resilient Floor Covering Institute (RFCI) Floor Score Program.

    - Standard Practice for The Testing Of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers, including 2004 Addenda.  California Department of Health Services.

  - SUBMITTALS

    - Product Data:  Submit manufacturer’s technical data for each type of resilient flooring and accessory.

      - Low Emitting Materials:

    - Submit manufacturer’s Material Safety Data Sheet Indicating VOC limits of all products.

    - Submit manufacturer’s certification that all adhesives and sealants comply with the GREENGUARD Product Emission Standard for Children & Schools or the Standard Practice for The Testing Of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers, including 2004 Addenda.  California Department of Health Services.

    - Submit manufacturer’s certification that all carpet products comply with the Resilient Floor Covering Institute (RFCI) FloorScore program.

      - Recycled Content:

        - Indicate recycled content; indicate percentage of pre-consumer and post-consumer recycled content per unit of product.

        - Indicate relative dollar value of recycled content product to total dollar value of product included in project.

        - If recycled content product is part of an assembly, indicate the percentage of recycled content product in the assembly by weight.

        - If recycled content product is part of an assembly, indicate relative dollar value of recycled content product to total dollar value of assembly.

      - Rapidly Renewable Content:

        - Indicate manufacturer and product name for each tracked material; total product cost for each tracked material; and percentage of product, by weight, for each material that meets the rapidly renewable criteria.

    - Samples for Initial Selection Purposes:  Submit manufacturer’s standard color charts in form of actual sections of resilient flooring, including accessories, showing full range of colors and patterns available, for each type of resilient flooring required.

    - Samples for Verification Purposes:  Submit the following samples of each type, color, and pattern of resilient flooring required, showing full-range of color and pattern variations.

      - Provide 4 samples of tile flooring of each color specified.

      - 2-1/2 inch long samples of resilient flooring accessories.

      - Other material as requested.

    - Certification for Fire Test Performance:  Submit certification from an independent testing laboratory acceptable to authorities having jurisdiction that resilient flooring complies with fire test performance requirements.

    - Maintenance Instructions:  Submit 2 copies of manufacturer’s recommended maintenance practices for each type of resilient flooring and accessory required.

    - Installer certification stipulated in paragraph F of Quality Assurance below.

    - Certification for Fire Test Performance:  Submit certification from an independent testing laboratory acceptable to authorities having jurisdiction that resilient flooring complies with fire test performance requirements.

    - Shop Drawing:  Provide accurately drawn plans at 1/4 inch = 1’-0” scale (min) indicating:  Gymnasium court layout including all striping; seaming layout and termination edging details with adjacent floor finishes.

  - QUALITY ASSURANCE

    - Manufacturers:  Provide each type of resilient flooring and accessories as produced by a single manufacturer, including recommended primers, adhesives, sealants, and leveling compounds.

    - Fire Test Performance:  Provide resilient flooring which complies with the following fire test performance criteria as determined by an independent testing laboratory acceptable to authorities having jurisdiction.

    - Critical Radiant Flux (CRF):  Not less than 0.45 watts per square cm per ASTM E 648.

    - Flame Spread:  Not more than 75 per ASTM E 84.

    - Smoke Density:  Not more than 450 per ASTM E 662.

    - Installer shall be certified by the manufacturer to insure warrantable installation.

  - PROJECT CONDITIONS

    - Maintain minimum temperature of 65 degrees F in spaces to receive resilient flooring for at least 48 hours prior to installation, during installation, and for not less than 48 hours after installation.  Store resilient flooring materials in spaces where they will be installed for at least 48 hours before beginning installation.  Subsequently, maintain minimum temperature of 55 degrees F in areas where work is completed.  Temporary HVAC is not acceptable.  System must be fully functional prior to resilient installation.

    - Install resilient flooring and accessories after other finishing operations, including painting, have been completed.  Do not install resilient flooring over concrete slabs until the latter have been cured and are sufficiently dry to achieve bond with adhesive as determined by resilient flooring manufacturer’s recommended Bond and Moisture test, pH test and Vapor Emission test.  Submit test results for owner’s review prior to the start of work.

- PRODUCTS

  - MANUFACTURERS

    - Subject to compliance with the specified requirements, provide products by the following manufacturer:

      - Manufacturers of resilient sheet flooring:

        - Flexco.

        - R. C. Musson Rubber Company.

        - (Basis of Design) The R.C.A. Rubber Company.

      - Manufacturer of Rubber Wall Base:

        - Burke Mercer Flooring Products; Division of Burke Industries, Inc.

        - Flexco Division, Textile Rubber Co.

        - Johnsonite.

        - Nora Systems, Inc.

        - Roppe Corporation.

        - VPI Corporation.

    - Substitutions:

      - Will be considered by the A/E and Owner when submitted per requirements of Division-0, Division-1, and Section 01630-Product Substitution Procedures.

    - All adhesive and sealant materials to comply with the Standard Practice for The Testing Of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers, including 2004 Addenda.  California Department of Health Services. or GREENGUARD Product Emission Standard for Children & Schools.

    - All resilient sheet flooring, rubber wall base, and stair tread/riser products shall contain recycled content.

  - MATERIALS-SHEET FLOORING

    - Rubber Sheet:  R.C.A. “Flexi-Flor” Sheet Rubber Flooring; ASTM F1859; 1/8 inch thick; 39 inch sheet width; 20 per cent minimum butadiene styrene rubber content by weight, non-staining, non-discoloring, and 100 per cent non-oil extended; hard clay filler, limestone filling not acceptable; asbestos-free; inlaid lines and striping of contrasting colors.  Color and pattern through total thickness, color as selected.

    - Striping:  Identical to R.C.A. “Flexi-Flor” sheet rubber flooring.

    - Custom floor pattern and color accent requirements are indicated on the Drawings.

    - Colors:  As selected by project consultant from manufacturer’s currently available range of standard colors only.

  - ACCESSORIES

    - Wall Base:  Provide preformed (a.k.a. molded) rubber cove base 6 inches high x 1/8 thick, standard toe, matte finish, complying with ASTM F1861, Type TS (thermoset), Style B (cove) installed lengths as long as practicable from roll stock; color as selected by consultant from manufacturer’s standard range of colors.

    - Neutralizing Agent:  One part muriatic acid to 9 parts water or 1 part vinegar to 5 parts water.

    - Subfloor Filler:  White premix latex; type recommended by flooring material manufacturer.

    - Adhesives:  R.C.A. No. 5 Epoxy Flooring Adhesive.

    - Edge Strips:  As specified in Section 09680-Carpet.

- EXECUTION

  - INSPECTION

    - Require Installer to inspect subfloor surfaces to determine that they are satisfactory.

      - A satisfactory subfloor surface is defined as one that is smooth and free from cracks, holes, ridges, coatings preventing adhesive bond, and other defects impairing performance or appearance.

    - Perform Moisture test, Hydrostatic Pressure test, Alkalinity pH test, and Bond test on concrete subfloor to determine if surfaces are satisfactory.  Perform 1 test each per 1000 gross square feet of building area.  Test locations to be determined by Owner’s representative.  Ensure that the following are achieved:

      - Moisture Content:  Maximum of 3 percent.

      - Hydrostatic Pressure:  Less than, or equal to, 3 pounds/1000 square feet/24 hours.

      - Alkalinity pH:  Less than 10 pH.

      - Bond:  achieved by 72 hours.

    - Beginning of installation means acceptance of existing substrate and site conditions.

  - PREPARATION

    - Use leveling and patching compounds as recommended by resilient flooring manufacturer for filling small cracks, holes and depressions in subfloors.  Tolerance: free of irregularities and level to within 1/8” in 10 feet.

    - Remove coatings from subfloor and lower wall surfaces that would prevent adhesive bond, including curing compounds incompatible with resilient flooring adhesives, paint, oils, waxes, and sealers.

    - Remove concrete curing compound completely.

    - Neutralize concrete floor surfaces.  Leave neutralizing agent on floors for minimum of 1 hour. Thoroughly flush and allow concrete to dry thoroughly (minimum 48 hours at 70 degrees F).

    - Broom clean or vacuum surfaces to be covered, and inspect subfloor.

    - Apply concrete slab primer, if recommended by flooring manufacturer, prior to application of adhesive.  Apply in compliance with manufacturer’s directions.

  - INSTALLATION-SHEET MATERIAL

    - Install in strict compliance with manufacturer’s printed instructions.

    - Spread only enough adhesive to permit installation of materials before initial set.

    - Set flooring in place, roll in both directions with 150 lb. Sectional roller to attain full adhesion.

    - Overlap edges of flooring.  Double cut seams.

    - Hand roll seams to force adhesive into seams to create chemical bond.

    - Lay flooring with joints, seams, court striping in accordance with approved shop drawings.

    - Terminate flooring at centerline of door openings where adjacent floor finish is dissimilar.

    - Install edge strips at unprotected or exposed edges, and where flooring terminates.

    - Scribe flooring to walls, columns, cabinets, floor outlets, and other appurtenances to produce tight joints.

    - Install flooring under moveable partitions without interrupting floor pattern.

    - Install edge strips where indicated.  Fit joints tightly.

  - INSTALLATION OF ACCESSORIES

    - Apply wall base to walls, columns, pilasters, casework and other permanent fixtures in rooms or areas where base is required.

      - Install base in lengths as long as practicable, with corners fabricated from base materials with mitered inside and outside corners.

      - Tightly bond base to substrate throughout length of each piece, with continuous contact at horizontal and vertical surfaces.

    - On masonry surfaces, or other similar irregular substrates, fill voids along top edge of resilient wall base with manufacturer’s recommended adhesive filler material.  Color of adhesive filler material is to match wall base color.

  - CLEANING and PROTECTION

    - Perform following operations immediately upon completion of resilient flooring:

      - Sweep or vacuum floor thoroughly.

    - Do not wash floor until time period recommended by resilient flooring manufacturer has elapsed to allow resilient flooring to become well sealed in adhesive.

    - Protection:

      - Protect resilient flooring against damage from rolling loads for initial period following installation by covering by covering with undyed, untreated building paper until inspection for Substantial Completion or hardboard where required to protect against loading or heavy traffic.  Use dollies to move stationary equipment or furnishings across floors.

      - Prohibit traffic on floor finish for 48 hours after installation.

  - EXTRA STOCK

    - Deliver stock of maintenance materials to Owner equal to 2 percent of amount installed of resilient sheet flooring, base and accessory item installed.

    - Furnish maintenance materials from same manufactured lot as materials installed and enclosed in protective packaging with appropriate identifying labels.

END OF SECTION