# SECTION 09705 (09 77 33)

## RESILIENT SAFETY WALL PADDING

GENERAL

SECTION INCLUDES

Protection wall padding (walls, floors, doors, frames, and ceilings) in time out rooms as indicated on the drawings and specified here in.

RELATED SECTIONS

06100-Rough Carpentry.

07270-Fire Stopping and Smoke Barrier Caulking.

08110-Steel Doors and Frames.

09125-Plastered Ceiling Suspension Systems

09215-Veneer Plaster.

09250-Gypsum Board.

REFERENCES

American Society for Testing Materials (ASTM):

D412-Vullanized Rubber and Thermoplastic Rubbers and Thermoplastic Elastomers-Tension.

D471- Rubber Property-Effect of Liquids.

D--- Rubber Property-Durometer Hardness.

E84-Surface Burning Characteristics of Building Materials.

SUBMITTALS

Product Data:  Submit manufacturer’s literature fully describing resilient padding and all related components, including standard details, published installation instructions, and maintenance recommendations.

Shop Drawings:  Submit complete shop drawings for specific installations indicated on the Drawings.

Samples:  Submit manufacturer’s standard range of wall panel colors and textures for selection by the Project Consultant.

After color and texture selection by Project Consultant, submit for final approval 12-inch square samples of wall panel and 6 inch long samples of related trim components including mounting hardware.

Maintenance instructions.

QUALITY ASSURANCE

Installer’s Qualification:  Shall have a minimum of 5 years experience in the fabrication and installation of resilient safety wall padding.

Fire Resistance Rating:  Materials and Construction must meet or exceed ASTM Class A Standards, as certified by testing, and inspecting organization acceptable to the authority having jurisdiction.

WARRANTY

Contractor shall agree to repair or replace any and all defective material or work for a period of 1 year from the date of substantial completion including:

Any Loss Adhesion.

Loss of Resilience.

Delamination.

PRODUCTS

MANUFACTURERS

Acceptable Manufacturers:  Subject to compliance with the specified requirements, provide products by the following manufacturer:

Marathon Engineering Corporation.

5615 2nd Street West

Lehigh Acres, FL

Tel:  (239) 303-7378.

Substitutions:

Will be considered by the A/E and Owner when submitted per requirements of Division-0, Division-1, and Section 01630-Product Substitution Procedures.

MATERIALS

Panel:  Gold Medal Safety Padding.

Protective padding material shall be synthetic resinous material.  Closed cell polyvinyl chloride or other types of polyvinyl surfacing will not be permitted.

All vertical panels shall be prefabricated, 1 inch nominal thickness, panel bonded on Oriented Stranded Board 7/16 inch thickness, making the total thickness 1-1/2 inch.

Door Jambs shall be 1/2 inch thickness gold Metal Padding with durometer of 60 plus or minus 5, for a total of 1 inch thickness.

Floor panels shall be prefabricated, 3/4 inch thick Gold Metal Padding bonded to Oriented Strand Board 7/16 inch thick for a total thickness of 1-1/4 inches.

PROPERTIES

Padding material in addition to meeting the minimum specified properties when cured shall also conform to the following criteria:

Flame Spread:  20.

Smoke Developed:  less than or equal to 450.

Weight shall be 5 lbs per square foot.

Tensile strength:  300-psi minimum in accordance with ASTM D412.

Temperature Stability:  Unaffected from 20 degrees to 120 degrees Fahrenheit.

Moisture Absorption:  0.8 percent to 1.05 percent by weight.

Compression Set:  90 percent recovery after 72 hours.

Compression Properties:  30 psi to 70 psi @ 50 percent modulus.

Elongation at Break:  150 percent (typ) per ASTM D412

Fungus Resistance:  100 percent.

Fasteners

As recommended by manufacturer.

EXECUTION

PREPARATION

The following conditions are required for installation and storage of materials:

General Contractor or Owner shall provide adequate ventilation.

A minimum temperature of 65 degrees F shall be maintained for the duration of the installation.

The General Contractor must provide 120-volt electrical service; storage in safe, warm, dry area; hoisting equipment and refuse receptacle.

INSTALLATION

Inspect surface to receive work under this section.

Grooves, cracks or other imperfections in the concrete shall be filled and leveled by the General Contractor.

Notify the Project Consultant and Owner in writing if surface/substrate is unsatisfactory for material application.  Commencement of work constitutes acceptance of surface

All concrete surfaces must have a 60 day cure.  No bonding agent or curing agent shall be allowed.

Vertical panels must be mechanically fastened to walls.

A minimum of 16 fasteners must be for 4 feet x 8 feet panel.

A gap of 1/8 inch plus/minus must be left between panels.  They will then be filled with Gold Metal Compound.  When fully cured, it will be sanded to meet adjacent edges.

All fastener holes must be filled with Gold Metal Compound and sanded.  Upon completion of all sanding of walls, doors, ceiling and floor, all surfaces must receive Gold Metal topcoat.

PRECAUTIONS

The following conditions are required for the installation and storage of materials.

General Contractor must provide adequate storage of materials.

A minimum temperature of 65 degrees F must be maintained for duration of installation.

General Contractor must provide 120-volt electrical service, storage in a safe, warm and dry area, hoisting equipment and refuse receptacle.

END OF SECTION