# SECTION 09705 (09 77 33)

## RESILIENT SAFETY WALL PADDING

- GENERAL

  - SECTION INCLUDES

    - Protection wall padding (walls, floors, doors, frames, and ceilings) in time out rooms as indicated on the drawings and specified here in.

  - RELATED SECTIONS

    - 06100-Rough Carpentry.

    - 07270-Fire Stopping and Smoke Barrier Caulking.

    - 08110-Steel Doors and Frames.

    - 09125-Plastered Ceiling Suspension Systems

    - 09215-Veneer Plaster.

    - 09250-Gypsum Board.

  - REFERENCES

    - American Society for Testing Materials (ASTM):

      - D412-Vullanized Rubber and Thermoplastic Rubbers and Thermoplastic Elastomers-Tension.

      - D471- Rubber Property-Effect of Liquids.

      - D--- Rubber Property-Durometer Hardness.

      - E84-Surface Burning Characteristics of Building Materials.

  - SUBMITTALS

    - Product Data:  Submit manufacturer’s literature fully describing resilient padding and all related components, including standard details, published installation instructions, and maintenance recommendations.

    - Shop Drawings:  Submit complete shop drawings for specific installations indicated on the Drawings.

    - Samples:  Submit manufacturer’s standard range of wall panel colors and textures for selection by the Project Consultant.

      - After color and texture selection by Project Consultant, submit for final approval 12-inch square samples of wall panel and 6 inch long samples of related trim components including mounting hardware.

    - Maintenance instructions.

  - QUALITY ASSURANCE

    - Installer’s Qualification:  Shall have a minimum of 5 years experience in the fabrication and installation of resilient safety wall padding.

    - Fire Resistance Rating:  Materials and Construction must meet or exceed ASTM Class A Standards, as certified by testing, and inspecting organization acceptable to the authority having jurisdiction.

  - WARRANTY

    - Contractor shall agree to repair or replace any and all defective material or work for a period of 1 year from the date of substantial completion including:

      - Any Loss Adhesion.

      - Loss of Resilience.

      - Delamination.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturers:  Subject to compliance with the specified requirements, provide products by the following manufacturer:

      - Marathon Engineering Corporation.

- 5615 2nd Street West

- Lehigh Acres, FL

- Tel:  (239) 303-7378.

    - Substitutions:

      - Will be considered by the A/E and Owner when submitted per requirements of Division-0, Division-1, and Section 01630-Product Substitution Procedures.

  - MATERIALS

    - Panel:  Gold Medal Safety Padding.

    - Protective padding material shall be synthetic resinous material.  Closed cell polyvinyl chloride or other types of polyvinyl surfacing will not be permitted.

    - All vertical panels shall be prefabricated, 1 inch nominal thickness, panel bonded on Oriented Stranded Board 7/16 inch thickness, making the total thickness 1-1/2 inch.

    - Door Jambs shall be 1/2 inch thickness gold Metal Padding with durometer of 60 plus or minus 5, for a total of 1 inch thickness.

    - Floor panels shall be prefabricated, 3/4 inch thick Gold Metal Padding bonded to Oriented Strand Board 7/16 inch thick for a total thickness of 1-1/4 inches.

  - PROPERTIES

    - Padding material in addition to meeting the minimum specified properties when cured shall also conform to the following criteria:

      - Flame Spread:  20.

      - Smoke Developed:  less than or equal to 450.

      - Weight shall be 5 lbs per square foot.

      - Tensile strength:  300-psi minimum in accordance with ASTM D412.

      - Temperature Stability:  Unaffected from 20 degrees to 120 degrees Fahrenheit.

      - Moisture Absorption:  0.8 percent to 1.05 percent by weight.

      - Compression Set:  90 percent recovery after 72 hours.

      - Compression Properties:  30 psi to 70 psi @ 50 percent modulus.

      - Elongation at Break:  150 percent (typ) per ASTM D412

      - Fungus Resistance:  100 percent.

    - Fasteners

      - As recommended by manufacturer.

- EXECUTION

  - PREPARATION

    - The following conditions are required for installation and storage of materials:

      - General Contractor or Owner shall provide adequate ventilation.

      - A minimum temperature of 65 degrees F shall be maintained for the duration of the installation.

      - The General Contractor must provide 120-volt electrical service; storage in safe, warm, dry area; hoisting equipment and refuse receptacle.

  - INSTALLATION

    - Inspect surface to receive work under this section.

    - Grooves, cracks or other imperfections in the concrete shall be filled and leveled by the General Contractor.

    - Notify the Project Consultant and Owner in writing if surface/substrate is unsatisfactory for material application.  Commencement of work constitutes acceptance of surface

      - All concrete surfaces must have a 60 day cure.  No bonding agent or curing agent shall be allowed.

    - Vertical panels must be mechanically fastened to walls.

    - A minimum of 16 fasteners must be for 4 feet x 8 feet panel.

    - A gap of 1/8 inch plus/minus must be left between panels.  They will then be filled with Gold Metal Compound.  When fully cured, it will be sanded to meet adjacent edges.

    - All fastener holes must be filled with Gold Metal Compound and sanded.  Upon completion of all sanding of walls, doors, ceiling and floor, all surfaces must receive Gold Metal topcoat.

  - PRECAUTIONS

    - The following conditions are required for the installation and storage of materials.

      - General Contractor must provide adequate storage of materials.

      - A minimum temperature of 65 degrees F must be maintained for duration of installation.

      - General Contractor must provide 120-volt electrical service, storage in a safe, warm and dry area, hoisting equipment and refuse receptacle.

END OF SECTION