# SECTION 09775 (09 77 43)

FIBERGLASS REINFORCED PANELS (FRP)

- GENERAL

  - SECTION INCLUDES

    - Fiberglass reinforced wall panels and accessories.

  - REFERENCES

    - American Society of Testing and Materials (ASTM).

      - D638-Tensile Properties of Plastic.

      - D695-Compressive Strength of Rigid Plastics.

      - D790-Prpoerties of Unreinforced and Reinforced Plastics and Electrical Insulating Materials.

      - E84-Surface Burning Characteristics of Building Materials.

    - Factory Mutual (FM).

    - Underwriters Laboratory (UL).

  - SUBMITTALS

    - Product Data:  Submit manufacturer’s literature fully describing fiberglass reinforced panels and all related components, including standard details, published installation instructions, and maintenance recommendations.

    - Shop Drawings:  Submit complete shop drawings for specific installations indicated on the Drawings.

    - Samples:  Submit manufacturer’s standard range of wall panel colors and textures for selection by the Project Consultant.

      - After color and texture selection by Project Consultant, submit for final approval 12-inch square samples of wall panel and 6 inch long samples of related trim components including mounting hardware.

  - QUALITY ASSURANCE

    - Provide panels that are FM approved and UL tested with a Flame Spread Class A rating under provisions of ASTM E84.

  - DELIVERY, STORAGE and HANDLING:

    - Store fiberglass reinforced panels indoors.

    - Store flat on skids.

    - Re-stack on a solid flat surface prior to installation.

- PRODUCTS

  - MANUFACTURERS

    - Subject to compliance with the specified requirements, provide products by one of the following manufacturers:

      - Crane Compostites-Kemlite, Glasbord.

      - Crane Composites-Sequentia, Inc., Stucto Glas FRP.

      - Marlite.

      - Nudo Products, Inc.,

    - Substitutions:

      - Will be considered by the A/E and Owner when submitted per requirements of Division-0, Division-1, and Section 01630-Product Substitution Procedures.

  - MATERIALS

    - Wall Panels:  Fiberglass reinforced plastic, minimum thickness 0.090 inches meeting the following performance criteria:

      - Size:  48 inches wide x 9 feet or 10 feet high depending upon ceiling height.

      - Weight:  0.6 pounds per square foot.

      - Interior Finish Class A

        - Flame Spread:  0-25.

        - Smoke Developed:  0-450.

      - Flexural Strength:  12000 to 15000 psi.

      - Tensile Strength:  8000 to 9000 psi.

      - Impact Strength (izod):  14.

      - Barcol Hardness:  55.

      - Water Absorption:  0.2 to 0.4 percent.

    - Accessories:

      - Trim Pieces:  Manufacturer’s standard 1 piece PVC moldings for panel joints, outside corners, inside corners, and end caps.

      - Fasteners:  Manufacturer’s standard nylon drive rivets.

      - Adhesives:  Latex-base construction adhesive as approved by the panel manufacturer.

      - Sealants:  Under provisions of Section 07920-Joint Sealants or LEED compliant silicone sealant as approved by panel manufacturer.

- EXECUTION

  - PREPARATION

    - Examine wall surfaces to receive fiberglass reinforced panels and conditions under which panels will be installed.

    - Do not proceed with installation of panels until surfaces and conditions comply with Manufacturer’s requirements.

  - INSTALLATION

    - Install fiberglass reinforced panels and trim pieces under provisions of Manufacturer’s published instructions.

    - Use panels with proper flexibility to conform to minor wall irregularities.

    - Allow for expansion at floors, ceilings and between panels.

    - Pre-drill oversize fastener holes.

    - Follow a precise pattern during fastening.

END OF SECTION