# SECTION 09965 (09 96 50)

## TEXTURED COATINGS

GENERAL

SECTION INCLUDES

Textured coating for tilt-up pre-cast concrete panels.

RELATED SECTIONS

03470-Tilt-Up Pre-Cast Concrete.

07920-Joint Sealants.

REFERENCES

American Society for Testing and Materials (ASTM):

B117-Operating Salt Spray (Fog) Apparatus.

D522-Mandrel Bend Test of Attached Organic Coating.

D968-Abrasion Resistance of Organic Coatings by Falling Abrasive.

D2243-Freeze-Thaw Resistance of Water-Borne Coating.

E84-surface Burning Characteristics of Building Materials

E96-Water Vapor Transmission of Materials.

G153-Conducting Accelerated Outdoor Exposure Tests of Coatings.

GREENGUARD Product Emission Standard for Children & Schools.

Green Seal Standard GS-03, Anti-corrosive paints, Second Edition, January 7, 1997.

Green Seal Standard GS-11, Paints First Edition, May 20, 1993.

South Coast Air Quality Management District (SCAQMD) Rule #1113.

Federal Test TT-C-555b-Resistance to Wind Driven Rain

SUBMITTALS

Product Data:  Submit manufacturer's technical information including label analysis and application instructions for each material proposed for use.

Copy of Warranty.

Wall Sample:

General:  For each coating system specified, provide a full height wall area between breaks as a wall sample for Project Consultant’s approval prior to beginning project application of each textured coating system.

Notify Project Consultant one week in advance of the dates and times when field samples will be ready for inspection.

Obtain Project Consultant’s acceptance.

Manufacturer's recommended application procedures that when approved by Project Consultant, will become the basis for accepting or rejecting actual application procedures used on the wall.

Low Emitting Materials.

Submit manufacturer’s Material Safety Data Sheet indicating VOC limits of all products.

Submit manufacturer’s for all products that comply with GREENGUARD Product Emission Standard for Children & Schools.

Submit manufacturer’s certification for all architectural paint, coating, and primer products applied to interior walls and ceilings that comply with the Green Seal Certification standard GS-11, Paints First Edition, May 20, 1993.

Submit manufacturer’s certification that all clear wood finish, floor coating, stain, sealer, and shellac products that comply with the South Coast Air Quality Management District (SCAQMD) Rule #1113.

Submit manufacturer’s certification for all anti-corrosive and anti-rust paint products applied to interior metal ferrous surfaces that comply with the Green Seal Standard GS-03, Second Edition, January 7, 1997.

QUALITY ASSURANCE

Applicator Qualifications:  Applicator shall be licensed in the State of Florida or in Broward County and use state or county journeymen.  Provide a legible copy of license and, when applicable a journeyman’s certification attesting to qualification requirements.

Certifications:  Paint applicator shall provide a certification attesting to having worked on projects similar in scope to this project for a minimum of 5 years.  Paint applicator not providing such documentation or not having the required experience will be removed from the project and replaced by the Contractor.

Source Limitations:  Obtain coatings from a single manufacturer.

All work shall be performed in accordance with referenced standards.

Coating system must be breathable, moisture resistant and comply with TT-C-555B Resistance to Wind Driven Rain.

DELIVERY, STORAGE, and HANDLING

Deliver materials to Project site in manufacturer's original, unopened packages and containers bearing manufacturer's name and label and the following information:

Product name or title of material.

Product description (generic classification or binder type).

Manufacturer's stock number and date of manufacture.

Application instructions.

Color name and number.

VOC content.

Container Labeling: Include manufacturer’s name, type of paint, brand name, brand code, coverage, surface preparation, drying time, cleanup, color designation, and instructions for mixing.

Store and mix materials in 1 area only.

Comply with health and fire regulations.  Take precautionary measures to prevent fire hazards and spontaneous combustion.

Lids must be kept tightly sealed.  Do not allow moisture to enter containers.

Store containers in a dry place, upright and airtight at temperatures of 45 degrees F and not exceeding one hundred 100 degrees F.  Skins formed on surface of material must be removed prior to moving containers, mixing or using.

PROJECT CONDITIONS

Apply coating only when temperature of surfaces to be coated and surrounding air temperatures are between 45 degrees F and 100 degrees F, unless otherwise permitted by manufacturer's printed instruction.

Do not apply over frozen surfaces, or when rain is imminent.

Incompatible substrate release agents, form oils, and any foreign material must be removed prior to priming and coating.

Roof and parapet top caps are installed and sealed against water penetration prior to priming and coating.

Primer shall not be exposed to ultra violet for more than 4 weeks prior to application of coating.  If exposure exceeds 4 weeks, primer shall be re-coated, as recommended by manufacturer.

Material use is above grade only.  Do not use below grade.

Joint Sealants must cure a minimum of 10 days or per manufacturer’s recommendation.  Excess sealant surface oils should be removed with an acetone solvent or approved cleaner.

WARRANTY

Provide limited commercial warranty for product replacement as aresult of defect in materials.  Notify manufacturer before product application.

Warranty:  Minimum 6 years.

PRODUCTS

MANUFACTURERS

Subject to compliance with the specified requirements, provide products by one of the following manufacturers:

BASF-Sonneborn; Product:  Super Colorcoat VOC (available in smooth and fine textures) and manufacturer approved primer.

BASF-Thoro; Product:  Thorocoat (available in smooth, fine, & coarse textures) and CM Primer.

(Basis of Design) Textured Coating of America, Inc.; Product:  TEX-COTE 300 (available in smooth, sand, fine, & coarse textures) and XL-70 “W” Primer.

Substitutions:

Will be considered by the Project Consultant and Owner when submitted per requirements of Division-0, Division-1, and Section 01630-Product Substitution Procedures.

MATERIALS

Concrete Coating System:

System:  Spray-on, high build, latex and acrylic copolymer resin, formulated to provide a weatherproof surface applied over concrete and masonry surfaces.

Textures:  As indicated on drawings or selected by Project Consultant.

Colors:  To be selected by Project Consultant from manufacturer’s standard colors and PPO standard colors

Performance Criteria:

ASTM G153:  Twin Arc Weatherometer:	5,000 hours.

Federal Test TT-C-555b-Resistance to Wind Driven Rain:		Passes.

ASTM D2243:  FreezeThaw Cycles:		250.

Wind-Driven Rain Test (98 MPH/24 Hours):	Passes.

Salt Spray Test ASTM B117:		300 hours

Abrasion ASTM D968 Falling Sand (Liters)-2,000 with 10% erosion:	Passes.

TTP-29:  21 Days–Fungus Growth Resistance:	Passes.

ASTM E84:					Passes.

ASTM E96:  				9.7 Perms.

ASTM D522:  				Passes 1 inch Mandrel.

VOC CONTENT

Products specified herein below must not exceed the following:

Interior Coatings (weight in grams/liter of product):

Non-Flat: 150.

Flat: 50.

Exterior Coatings weight in grams/liter of product minus water):

Non-Flat: 200.

Flat:  100.

EXECUTION

EXAMINATION

Applicator must examine areas and conditions under which textured coating work is to be applied and notify Contractor in writing of conditions detrimental to proper and timely completion of work.  Do not proceed with work until unsatisfactory conditions have been corrected in a manner acceptable to applicator.  Start of coating operation implies acceptance of the surface conditions and responsibility for required standards and appearance.

SURFACE PREPARATION

General:  Perform preparation and cleaning procedures in accordance with coating system manufacturer's printed instructions and as herein specified, for each particular substrate and coating condition.

Remove hardware accessories, machined surfaces, plates, lighting fixtures and similar items in place and not to be finish-coated or provide surface applied protection prior to surface preparation and coating operations.  Remove, of necessary, for complete coatings of items and adjacent surfaces.  Following completion of coating of each area, reinstall removed items.

All surfaces shall be sound and clean prior to application of primer and coatings.  Such surface contaminants as dust, dirt, mildew, form oils, loose substrate, etc., shall be removed by waterblasting.  Excessive form oils, release agents and curing compounds may require light sandblasting.

Cracks:

Patch per manufacturer’s written instructions using manufacturer approved repair products.

Finish of patching compound shall match finish of adjacent surfaces.

Mask all glass, shubbery and asphalt surfaces.

Over a primed, clean and sound surface apply textured coating at standard coverage rate in selected texture and color.

Application Rate:  Provide pinhole-free membrane for moisture resistant integrity, uniform thickness over the entire surface being covered.  Apply at dry film thickness (DFT) and number of coats necessary to achieve the texture selected and to be moisture resistant.

Curing Time:  Twenty-four hours minimum.

INSTALLATION

Apply coating in accordance with manufacturer's directions.  Use applicators and techniques best suited for substrate and type of material being applied.

Concrete System:

Over a primed, clean and sound surface apply textured coating at standard coverage rate in selected texture and color.

Application Rate:

          - Provide pinhole-free membrane for moisture resistant integrity, uniform thickness over the entire surface being covered.  Apply at dry film thickness (DFT) and number of coats necessary to achieve the texture selected and to be moisture resistant.

          - Minimum dry film thickness of primer and finish coat(s) shall total 13-15 mils.

Curing Time:  Twenty-four hours minimum.

Application of textured coating shall be a uniform film thickness over entire surface being covered.

A wet edge shall be maintained to prevent lapmarks.

Avoid starting and stopping midway on wall.  Continue to a natural break such as a panel edge or corner.

CLEANING and PROTECTION

Clean-up:  During progress of work, remove from site discarded coating materials, rubbish, cans and rags at end of each work day.

Upon completion of coating work, clean window glass and other coating-splattered surfaces.  Protect work of other trades, whether to be coated or not, against damage by coating and finishing work.  Correct any damage by cleaning, repairing or replacing, and recoating, as acceptable to Project Consultant.

Provide "wet paint" signs as required to protect newly-coated finishes.  Remove temporary protective wrappings provided by others for protection of their work, after completion of coating operations.

At the completion of work of other trades, touch-up and restore all damaged or defaced surfaces.

END OF SECTION